SECTION 07 71 19
MANUFACTURED GRAVEL STOPS AND FASCIA
PART 1 - GENERAL

1.01
RELATED DOCUMENTS
A. The provisions included under Division 1, General Requirements, are included as part of this section as though bound herein.

1.02
SUMMARY

A. Provide labor, material, and equipment necessary for furnishing a complete installation of commercial gutter system.

B.
Related Work Specified Elsewhere

1.
Division 4 Sections for masonry.

2.
Division 6 Sections for nailers and support framing.
3.
Division 7 Sections for related roofing materials.

1.03
SUBMITTALS

A. Product Data: Each type of product specified. Submit manufacturer's detailed technical product data, installation instructions and recommendations, dimensions of individual components, profiles, and finishes

B. Shop Drawings: Show fabrication and installation of parapet copings including fully dimensioned roof plans, expansion joint locations, sections and details of components and other related trims.

C. Finish & Color Selection: Furnish manufacturer's technical data for specified finish and color chart showing full range of colors available.

1.04
QUALITY ASSURANCE
A. Where pre-engineered manufactured products are specified, other field fabricated or shop/field fabricated substitutions will not be accepted. However, where shop/field fabrications are indicated pre-engineered systems will be considered with Architect approval.

B. Obtain all components and related accessories from one single source manufacturer.

C. Follow manufacturer's printed instructions for installing parapet copings. If copings join a roof system then follow primary roofing manufacturer's printed instructions for installing associated roof material for flashing parapets and coping.

1.05
DELIVERY, STORAGE & HANDLING
A. All products delivered shall be stored in a clean dry location prior to installation.

B. Products furnished with strippable protective masking shall not be exposed to direct sunlight for more than 30 minutes without removing masking.

C. Do not install finished materials with scars or abrasions.
1.06
PROJECT CONDITIONS
A. Coordinate work of this Section with adjoining work for proper sequencing to ensure protection from inclement weather and to protect materials and their finish against damage.

B. Do not install copings during inclement weather. When installing in cold climates, warm adhesives, caulks, and primers to at least 50 degrees Fahrenheit prior to application.

PART 2 PRODUCTS

2.01
MANUFACTURERS
A. Provide manufactured gravel stop system and accessories as manufactured by Perimeter Systems, a division  of Southern Aluminum Finishing Company, Inc. 14100 Veterans Memorial HWY, Villa Rica, GA  30180, (800) 334-9823, Online at http://www.saf.com/persys
2.02 TYPE

A. Provide Perimeter Systems' Press-Loc® Gravel Stop System, Geometric Collection, 
6” Size, Model Number PLGS.GC3-6.
2.03
MATERIALS & FABRICATION
A.  Gravel stop snap on decorative fascia shall be manufactured from 0.040" aluminum, 10'-0" lengths. Fascias shall be press formed with required dies on a CNC Press to provide repeated true and accurate profiles. 
B. Fascia Splices shall be manufactured from 0.040" aluminum, 4" lengths, formed to fit the inside of snap on fascia.
C. Continuous cleat to be manufactured from 0.085” 6063-T5 aluminum extrusion.
2.04
ACCESSORIES
A. Mitered Corners: Provide factory mitered corners. Facia profiles shall be precision saw cut with a continuous heliarc weld to produce a watertight joint.

B. Sculptured End Caps: Provide factory mitered end caps for fascia. Fascia profiles shall be precision saw cut with a continuous heliarc weld to produce a watertight joint.
2.05
FINISHES
A. General: Apply coatings to exposed aluminum components after fabrication for maximum coating performance and to prevent crazing, abrasion, and damage to finished surfaces.

B. Pretreatment: Aluminum components shall be pretreated with solutions to remove organic and inorganic surface soils, remove residual oxides, followed by a chrome phosphate conversion coating to which organic coatings will firmly adhere.

C. Coating Type: High Performance Coating, two-coat, shop applied, 70% Polyvinylidene Fluoride (PVDF) coating based on Elf Arkema Chemicals, Inc. Kynar 500 or Ausimont U.S.A., Inc. Hylar 5000 resin, meeting AAMA 2605 specification.

D. Color: Select from manufacturer's full range of 56 EZ Mix Colors.
PART 3 EXECUTION

3.01
EXAMINATION
A. The installer must examine substrates and conditions under which gravel stops will be installed. All wood plates shall be installed true, straight, and free of splits, cracks, or other irregularities. Do not proceed with installation until unsatisfactory conditions are corrected.

3.02
INSTALLATION
A. General: The gravel stop system shall be installed in strict accordance with manufacturer's printed instructions. Deviations from the instructions are not allowed.

B. Fastening: Gravel stop shall be snapped onto continuous cleats according to manufacturer’s instructions. Cleat shall be fastened with #12 x 1 ½” stainless steel wood screw.
C. Install fascia concealed splice plates at all fascia joints. Splice plate shall be sealed with a non-hardening, low modulus, sealant as recommended by coping manufacturer.
END OF SECTION 07 71 19
